Coadd™ D-6290

Dispersant

DESCRIPTION

Coadd™ D-6290 is a specialized polymer dispersant for water-based coatings, capable of stabilizing effect pigments. It aids in the orientation of effect pigments, and when used in conjunction with orientation agents, it can achieve enhanced surface effects. It is universally applicable to both resin-free and resin-containing pigment paste systems. This product is also suitable for the dispersion systems of water-based inorganic and organic pigments, enhancing the stability and color development of the pigment systems.

PHYSICAL PROPEERTIES

| Appearance | Yellow to amber liquid |
| --- | --- |
| Density（g/ml） | 0.99 |
| Active content (%) | 100 |
| Viscosity (25°C, mPas) | <1500 |

Note：These properties are only typical, and do not represent product specifications

APPLICATION CHARACTERISTIC AND ADVANTAGES

Coadd™ D-6290 is suitable for water-based metal, leather, and plastic coatings, particularly effective for the dispersion of effect pigments, significantly improving stability and orientation. It is recommended to be added at 10-40% based on the effect pigments.

In systems co-grinding inorganic and organic color pastes, the addition rate is 5-50% depending on actual needs, aimed at enhancing stability and color development. This product is a 100% polymer content. Under reduced temperatures, it may exhibit increased viscosity and partial crystallization; however, upon warming, it returns to its original viscosity. It can be used directly without affecting product performance.

Above dosage are only for orientation, optimum level of dosage should be determined via laboratory tests.

SAFETY NOTICE

Before using the products, please refer to SDS for detailed safety data, handling and storage procedures recommended.

DISCLAIMER

It is common proposal for product usage and demand above information based on our professional knowledge. Due to environmental uncertainty and out of our control from practical process, please test and make evaluation ahead of use to ensure efficient and safe. For your reference, the above information is only for commonly known and use the product. It is guaranteed to meet quality and product specification.

**Please refer to SDS for more information