Coadd™ DO-6269

Dispersing Agent

DESCRIPTION

Coadd™ DO-6269 is a mixture of polyacrylic block polymer with pigment affinity groups, and is suitable for solvent-borne and solvent-free coating systems. The product is a universal wetting and dispersing agent, with excellent viscosity reduction properties. It can be used to disperse both organic and inorganic pigments, especially suitable for carbon blacks. The product can be used in the grinding of resin containing and resin free colorant systems, and solvent-borne coatings with high solid content.

PHYSICAL PROPEERTIES

| Appearance | Light yellow liquid |
| --- | --- |
| Density（g/ml） | 0.96 |
| Active content (%) | 30 |
| Viscosity (25°C, mPas) | <1000 |

Note：These properties are only typical, and do not represent product specifications

APPLICATION CHARACTERISTIC AND ADVANTAGES

Coadd™ DO-6269 is recommended for different kinds of resin and pigmented systems, with excellent compatibility. Especially effective in dispersing carbon blacks, to reduce the system viscosity. Solidification may occur temperature is low, please warm up and mix well before use.

Suggested dosage (base on the pigment volume):

Titanium oxides: 2 – 5%

Organic pigment: 15 – 40%

Inorganic pigment: 5 – 40%

Carbon black: 40 – 100%

Above dosage are only for orientation, optimum level of dosage should be determined via laboratory tests.

SAFETY NOTICE

Before using the products, please refer to SDS for detailed safety data, handling and storage procedures recommended.

DISCLAIMER

It is common proposal for product usage and demand above information based on our professional knowledge. Due to environmental uncertainty and out of our control from practical process, please test and make evaluation ahead of use to ensure efficient and safe. For your reference, the above information is only for commonly known and use the product. It is guaranteed to meet quality and product specification.

**Please refer to SDS for more information